## Slide 1
Advancement of High Gradient Study at 100MV/m Range
肥後寿泰,松本修二、横山和枝、福田茂樹,
東保男, 高富俊和、上野健治
KEK
100MV/m級高電界加速試験の進展

## Slide 2
要旨
TeV以上のリニアコライダーに必要な100MV/m級の高加速勾配を目指す基礎技術研究として、CLIC用加速管のプロトタイプ、20㎝級進行波型加速管に対する高電界試験
ダンピング構造を付加すると放電頻度が二桁上昇
試験加速管は通常通り製作・試験：
KEKによるセルの製作、SLACによる化学研磨、水素ロウ付け、真空ベーキング
 2台ペアで製作し、一台はKEK（Nextef）で、一台はSLAC（NLCTA）で試験
ダンピング構造入り口で磁場極大部に、火山の硫黄ガス噴出部に見かける
噴出孔構造を発見
磁場を抑えたパラメータの加速管、
T24（ダンピング無し）はT18以上に放電頻度が少ない（KEK）
震災により空気でパージされた後は、放電頻度が上昇、
放電場所は変わらず加速管内で一様分布
9月から、ダンピング構造を持つTD24型加速管の試験を進める。
T18→T24 のBDR減少に対応して低いBDRを示すか？ を注目

## Slide 3: 加速管パラメータ Unloaded 100MV/m T18, T24 TD18 Un-damped Heavily damped
P (MW), Es (MV/m), Ea (MV/m), DT(C), Sc*50 (MW/mm2)
Iris number
P
Ea
Sc
Es
DT
T18 unloaded
100MV/m
P (MW), Es (MV/m), Ea (MV/m), DT(C), Sc*50 (MW/mm2)
Iris number
P
Ea
Sc
Es
DT
TD18 unloaded
100MV/m
DT~47C

## Slide 4: T24  TD24
Idea is to reduce Hs in TD24 comparing to TD18.
P
DT
Sc
Ea
Es
P
DT
Sc
Ea
Es
DT<25C
Tested To be tested

## Slide 5: Processing whole history
TD18
Damped
T18
Undamped
T24
Undamped
ACC-BD=7000
ACC-BD=1100
ACC-BD=2000
RF ON=4000hr
RF ON=3000hr
RF ON=1700hr
Dec.2010-Mar.2011
Dec.2009-Nov.2010
Oct.2008-Jun.2009
100MV/m
ダンピング構造無しの加速管は全放電数が少ない

## Slide 6
Comparison of dark current
T18_Disk
TD18_Disk
Eacc for peak dark current of 10 mA
90MV/m 70MV/m 85MV/m
T24_Disk
Undamped 85~90 MV/m damped ~70MV/m
暗電流の少ない方が高電界特性が良い？

## Slide 7: 放電頻度の比較 及び 変遷
比較Damped
Undamped
BDR変遷
T18 Eacc依存性
TD18 Eacc依存性
ダンピング有りは無しに比べて放電頻度が二桁高い

## Slide 8: T24#3 BDR evolution at 252ns normalized 100MV/m
Assuming the same exponential slope as that at 400hr
放電頻度：T24は少ない＆は減り続ける
BDR変遷

## Slide 9
Near iris
SEM inspection by CERN on eq. acc structure, TD18#3
Markus Aicheler 13. Oct. 2010
放電の痕跡
ビーム径アイリス近傍には放電痕多数確認

## Slide 10
TD18_Disk
高BDRへのトリガー可能性＠高Hs
Milling + Turning + Light etching < 1mm
Hs maximum point
Near max Hs
SEM inspection by CERN on eq. acc str, TD18#3
Markus Aicheler 13. Oct. 2010
Hs max
Pulse heat damage
高磁場点の多くに不可思議な形状が出現
放電トリガーの可能性？

## Slide 11
配置
１
2
3
4
10
5
6
9
8
7