## Slide 1: Results from Nextef Observations in high gradient tests of CLIC Prototype Structures and associated study activities
CLIC2013, CERN
29 January, 2013
T. Higo (KEK)

## Slide 2: Contents
Summary on CLIC prototypes
  The most recent result on TD24R05
  Comparison
    Ramping speeds
    Breakdown rates
  Hot spots
Further studies in Nextef

## Slide 3: Nextef for high gradient R&D
KT-1
X-band
KT-2
C-band
Nextef
X-band
A
B
KT1-B
Nextef Control

## Slide 4
A
B
Control
RF source for A
Nextef
Shield A
Shield B

## Slide 5: High gradient tests of CLIC prototype structures
Collaboration from 2007 ---
 T18#2 2008 --- 2009
 TD18#2 2009 --- 2010
 T24#3 2010 --- 2011 IWLC2011 Granada
 TD24#4 2011 --- 2012 LWLC2012 Arlington
TD24R05#2 2012 --- 2013 CLIC2012 Geneva
TD24R05#4 2013 ---

## Slide 6: High-gradient test at Nextef
Basic studies at shield-B
TD24R05 #2
TD24_Disk_#4
High power components test
KT1 to shield-B
TD24R05 #4?
TD24R05(KEK)?
Replace klystron
T18_Disk_#2
TD18_Quad_#5
TD18_Disk_#2
Narrow waveguide test
KT1
Nextef
KX03 (60cm HDDS)
T24_Disk_#3
4 7 10 1 4 7 10 1 4 7 10 1 4 7 10 1 4 7 10 1 4 7 10 1
2008 2009 2010 2011 2012 2013
Shield-B
CLIC prototype tests
GLC
1
2
3
4
5
1.5

## Slide 7: Reduce Hp/Ea and DT by reducing corner radius in the cell
TD24
TD24R05
Alexej Grudiev

## Slide 8: What to be studied in mind with the most recent test with TD24R05
Prove the CLIC high gradient feasibility
Undamped  well done in T24
Prove with damped structure
Ramping speed
BDR at 100 MV/m
Evolution of BDR vs time
BDR vs Eacc
BDR vs width
Robustness against long-term operation

## Slide 9: Preparation always follow our nominal structure fabrication flow

## Slide 10: CLIC test structures; fabrication and test T18 TD18T24TD24TD24R05
1. T18_Disk_#2
2. TD18_Disk_#2
3. T24_Disk_#3
4. TD24_Disk_#4
5. TD24R05 under test now
undamped
damped

## Slide 11: SLAC/KEK typical fab/test flow
Design for CLIC (CERN)
Fabrication of parts (KEK)
Bonding (SLAC)
CP (SLAC)
VAC bake (SLAC)
High power test (NLCTA-SLAC)
High power test (Nextef-KEK)
Notes: プロトタイプの試験サイクル
ここでも 日米を基礎におく SLAC・KEK キープレーヤー

## Slide 12: TD24R05 and Comparison in initial processing

## Slide 13: TD24R05#2 Processing history

## Slide 14: TD24R05 Eacc versus #ACC-BD

## Slide 15: Difference in processing speed among 5 disk-stack-type CLIC-prototype structures
T24
T18
TD18
TD24
51ns
91ns
132ns
TD24R05
Number if ACC-BD’s until reaching the same level in (Tp, Eacc)
Speed
1. T24
 2. TD24R05
 3. T18
 4. TD24
 5. TD18
Still to be revised for better comparison (130126)

## Slide 16: Breakdown rate in flat pulse operation

## Slide 17
TD24R05 less steep as Eacc than TD24.
To be evaluated in a better experimental situation and possibly at later times.

## Slide 18
T24#4
(final)
TD24#4
(~2000hrs)
BDR summary on TD24
comparing to T24
Arlington presentation
+ typical present

## Slide 19: Similar to TD24 but deteriorated at 1700hrs during long-pulse?
Run 31
Run 29

## Slide 21
The same as TD24 in the early stage with hot spots appeared.
Curious to see how it goes eventually.

## Slide 22: BDS vs width
Width dependence measured
At time from RF-ON about 1600 hours
Typical and similar to those before.
Worthwhile to compare among those carefully but this work is underway.
Longer pulse may make the situation bad, as seen in TD24R05.

## Slide 23: Appearance and disappearance of hot spots

## Slide 24: Hot spots have appeared
Run 11
706—787 hrs
BD cell
Run 31
2122—2169 hrs
Run 27
1797—1863 hrs
Downstream
Upstream
No bad cell

## Slide 25: Hot spots localized in each cell
Run 31 at 110 MV/m
Run 27 at 100 MV/m
Only downstream
Both up and down

## Slide 26: Run 32 run at 105 MV/m one of the sports disappeared
Dominant
BDR = 4.2 X 10 -6
A little decreased
due to disappearance of BD upstream?
Gone?

## Slide 27: TD24R05#2 Processing history
Non
BDR increase

## Slide 28: Hot spots
Spots appeared after long-pulse operation.
They appear and disappear. The appearance may depend on field level, pulse width, etc.
We want to see how spots behave in further operation.
This is the first time for us to notice such hot spots, out of 5 prototype structures. Some cases known also at SLAC tests.
We need to identify the source of such spots and establish the technology to be away from them.

## Slide 29: What to do for linear collider?
Evaluate performance and find mechanism
Just suppress it
  Material?
    Inclusion, foreign material, or crystal defects, ….
  Fabrication process?
    Clean environment
    Escape from possible dirty process, ….
  Processing in practice
    Any protocol?, gentle processing?,

## Slide 30: Setups being prepared to study characteristics and mechanism of vacuum breakdowns in RF

## Slide 31: Single-cell studies in preparation or in mind
Explore basic research in a simple geometry
Center cell is such as the following
  Standard: KEK made – SLAC test
  Nominal: Heavily-damped
  Made of large-grain material
  Undamped but all-milled
  All milled quadrant type
  Choke-mode type
These are under preparation
HG2012 in April 2012
Notes: 継続申請の3年間の目標 概略
基礎試験の立ち上げ
複合材料を含めた試験
TWでの可能性 見極め
放電頻度を決める放電のトリガーの理解
100MV/m超の加速ユニットの提案

## Slide 32: Study with simple-geometries
Need to identify the breakdown mechanism in the relevant field level and including initial processing stage
Key issue toward stable high gradient operation for large-scale machine as CLIC
Studies with both prototype structures and simpler geometries are needed
KEK prepared the second test area (“Shield-B”) for the latter
Almost ready to start, just waiting for the klystron replacement

## Slide 33: Strategy in mind
Proceed to evaluate
Damped cell
Damping aperture shape
Material
HIP, …..
Fabrication
Turning vs Milling
Heat treatments
Etching
Geometry
Quad
Choke
Start with a single-cell setup in nominal design and nominal fabrication method

## Slide 34: Quad with large Chamfer (R=400mm) with single-cell setup
To understand why quad-type does not perform well under high gradient and possibly cure the problem!?
Shield-B
R=400mm
(Round Chamfer)
0.1mm gap
between
facing planes

## Slide 35: Field Enhancement due to the Concave Structure
Copper
Vacuum
Numerically Calculated by the Floating Random Walk Method
with Accuracies Better than 0.5%
For more details, see
T. Abe, “Study of Surface Field Enhancements due to Fine Structures,”
presented at the 8th Annual Meeting of Particle Accelerator Society of Japan, 2011 ,
Paper ID:TUPS086.
|E| or |H|
E.g.

## Slide 36: On-going copper surface evaluation
End mill
Ball End mill
Turning lathe
Scratch by profilemeter
Takatomi

## Slide 37: Heat deposit by laser and probed with SR light
SR X-ray
Drive laser

## Slide 38: Crystal evaluation by PF X-ray
Laser irradiation -> time dependent angle shift
of X-ray Bragg reflection (X. Zhang)
Before
33nsec delay
After delay
Shift corresponds to 300 degC
Zhang

## Slide 39: Parameters and next experiment
Experimental parameters
  Laser:
    YAG-Laser, pulse width 6~8ns,10Hz
    Power:0.5mJ/shot~10mJ/shot
  Probe beam diameter:
    x-ray: 60mm, laser:100 mm
  Time resolution:
    6ns
February experiment
  Evaluate relaxation time of material
  Irradiation limit for material to mechanically respond
  Crystal disruption limit versus power density and cycles of irradiation

## Slide 40: Efforts to keep and develop RF power source for Nextef

## Slide 41: RF power sources
Modulator
  Invertor HV supply robust
  Thyratron needs intermittent adjustment or failure
PPM Klystrons
  Three have been used for nearly 10 years
  Pulse shortening exists
  But survives at 40MW level
  Failure in water circuits
  Not RF-origin failure
Driver for klystron
  Semiconductor amplifier

## Slide 42: Effort to re-activate fabrication engineering lead by KEK

## Slide 43: Continue fine parts fabrication +
DDS
12 GHz damped-detuned cells were made
By KEK
Takatomi
An example

## Slide 44: Assembly at KEK and surroundings An idea under consideration
High temperature processing
VAC baking eq.
Close Stainless steel vessel
and extract to clean room?

## Slide 45: In conclusion

## Slide 46: CERN/KEK collaboration has kept the base for KEK’s R&D toward high gradient
KEK
Structure fabrication & test @Nextef
CERN supports for structure fabrication, high power test & system expansion
SLAC conducts structure fabrication, high power test & basic research
US-Japan
SLAC/KEK
CERN/KEK collaboration
CLIC
US-HG
Tsinghua, IHEP
Structure design, fabrication & test
Asian collaboration
Medical
Industrial
Higgs, and others
Application

## Slide 47: Summary
Six CLIC prototypes tested at Nextef
Breakdown rate proven in TD24#4 with CLIC pulse
TD24R05 found smoothly processed but hot spots emerged
Further studies in simple setup is almost ready
RF power sources are to be reinforced
CLIC high gradient collaboration keeps X-band study at KEK active
KEK further aggressive activities are foreseen after commissioning of SuperKEKB in early 2015